DETAILS OF THE CONDUCTIVE

General :

Minimum conductor width (inner and outer)		: 0.120 mm

Minimum spacing between conductors (i and o)	: 0.120 mm

DIMENSIONS OF VIAS

Plated through via's:

Designed hole diameter		: 0.200 mm

Tolerance on finished hole diameter		: none

Copper land diameter		: 0.400 mm

Minimum copper thickness into plated through via’s	: 0.015 mm

PCB STRUCTURE

Number of layers		: 4

Total thickness  min		: 1.584 mm

Copper 1 final thickness....................................................	0.042 mm (0.017mm Cu + Plating)

Epoxy 1 basis thickness (core)......................................  	0.150 mm

Copper 2 final thickness....................................................	0.017 mm

Epoxy 2 basis thickness (core)......................................  	1.160 mm

Copper 3 final thickness....................................................	0.017 mm

Epoxy 3 basis thickness (core)......................................  	0.150 mm

Copper 4 final thickness....................................................	0.042 mm (0.017mm Cu + Plating)

SOLDER RESIST SPECIFICATION

-----

(Copper : Red   –   Solder Resist : Green)

Thickness A : NA

Thickness B : NA

Thickness C : NA

FINISHING

Ni + Au, thickness 5 +4/-2µm electroless Ni and 0.1 +0.05/-0.05 µm immersion Au

MATERIAL

Dielectric permittivity: 4.3

Solder resist permittivity: 3.4

All material MUST be compatible with Lead Free process and compatible with ROHS directive.

IMPEDANCES REQUIREMENTS:

Single-ended

| Layer | Track width | Distance between diff tracks | Isolation to gnd | Impedance Requested | Reference |
| --- | --- | --- | --- | --- | --- |
| Layer 1 (RF) | 560um | - | 120um | 50 Ohms | Layer 3 |
| Layer 1 (RF) | 260um | - | 310um | 50 Ohms | Layer 2 |

STRATEGIC PADS AND TRACKS:

N/A

BOW (before and after reflow)

Acceptable bending => A under or equal		: 1.5 mm

1

TWIST (before and after reflow)

Acceptable twist is lower or equal		: 1.5 mm

BOW + TWIST(before and after reflow)

Accept. bow + twist sum is lower or equal		: 1.5 mm